# LBP11.01 Super Fine Lime Putty					  Product Data Sheet

| ## Description | Fine grade non-hydraulic lime putty slaked from Buxton Calbux 90M quicklime. The putty is matured for a minimum of 3 months. |
| --- | --- |
| Health & Safety | Calcium Hydroxide Ca(OH)² Alkali (pH 13). Cas No 1305-62-0. EINECS No 215-137-3. Danger: H318 Causes Serious Eye Damage Warning: H315 Causes skin irritation STOT SE3 H335 May cause respiratory irritation See Safety Data Sheet - LBP11 Lime Putty |
| Environmental Considerations | Lime putty is an environmentally sustainable product made from natural ingredients. It contains no VOCs and no petrochemical products. |
| ## Uses | Used in fine finish top-coat lime plasters when it is mixed with a fine sand normally at 1:1 or 2:1, and for lime/gypsum blend finish plasters. Superfine grade putty is used in the manufacture of Sheltercoats and can be diluted with water and used as an internal limewash. Superfine lime putty is used in ‘fine conservation’ generally. |
| ## Availability | 21 litre (28kg) tubs. |
| ## Shelf Life | Matures and improves with age when kept in sealed containers. Protect from frost. |
| ## Observations | Tradesmen familiar with the use of lime putty, and with experience of its successful use should be employed. Accurate volumetric site mixing is essential. Non-hydraulic limes do not perform as gypsum plaster or modern hydraulic lime. Non-hydraulic lime sets only by reaction with atmospheric carbon dioxide in the presence of moisture. This ‘carbonation’ is a slow process and control of the drying and setting process by tending and protecting is crucial to success and long term performance. Do not use in temperatures of 5ºC and falling. Protect from frost. |
| Technical Advice | From our Technical Department on 01460 281921 Email: info@limebase.co.uk Limebase Products Ltd Walronds Park Isle Brewers Taunton Somerset TA3 6QP All products data and H&S sheets can be printed from our web site: www.limebase.co.uk |
|  | August 2016 |