# LBP11.02 Chalk Lime Putty					 	    Product Data Sheet

| ## Description | Mortar grade non-hydraulic lime putty slaked from Singleton Birch Lincolnshire chalk burnt at C.1000ºC. The creamy-white putty is matured for a minimum of 3 months, and contains a small proportion of <3mm flint and un-burnt chalk particles. |
| --- | --- |
| Health & Safety | Calcium Hydroxide Ca(OH)² Alkali (pH 13). Cas No 1305-62-0. EINECS No 215-137-3. Danger: H318 Causes Serious Eye Damage Warning: H315 Causes skin irritation STOT SE3 H335 May cause respiratory irritation See Safety Data Sheet - LBP11 Lime Putty |
| Environmental Considerations | Lime putty is an environmentally sustainable product made from natural ingredients. It contains no VOCs and no petrochemical products. |
| ## Uses | To be mixed with sands, stone dusts and aggregates normally at 1:2½ or 1:3 by volume (depending on application) to produce lime putty bedding and pointing mortars and internal base coat plasters. Pozzolans are normally added on site for external renders, and work in exposed locations. Seek technical advice. |
| ## Availability | 21 litre (28kg) tubs. |
| ## Shelf Life | Matures and improves with age when kept in sealed containers. This putty will stiffen during maturation, but can be plasticised without the addition of water by thorough mixing. Protect from frost. |
| ## Observations | Tradesmen familiar with the use of lime putty, and with experience of its successful use should be employed. Accurate volumetric site mixing is essential. Lime putty mortars do not perform as gypsum, cement, or hydraulic lime. Non-hydraulic lime sets only by reaction with atmospheric carbon dioxide in the presence of moisture. This ‘carbonation’ is a slow process and control of the drying and curing process by tending and protecting is crucial to success and long term performance. Do not use in temperatures of 5ºC and falling. Protect from frost. |
| Technical Advice | From our Technical Department on 01460 281921 Email: info@limebase.co.uk Limebase Products Ltd Walronds Park Isle Brewers Taunton Somerset TA3 6QP All products data and H&S sheets can be printed from our web site: www.limebase.co.uk |
|  | August 2016 |