Finelime® 2

EN 459-1 CL 90-Q (R5, P4)

High Calcium Quicklime - Calcium Oxide CaO

Finelime is a coarse, white calcium oxide powder which is made by crushing and screening quicklime.

Typical		Specification

Chemical Analysis     (Dry Basis)				% Mass		% Mass

Calcium oxide			CaO			94			90.0 min

Silica				SiO2			1.9

Magnesium oxide		MgO			0.42			5.0 max

Aluminium oxide		Al2O3			0.23

Ferric oxide			Fe2O3			0.13

Carbon			CO2			2.6			6.0 max

Sulphur			SO3			0.04			2.0 max

Physical Analysis

Reactivity 			Time (Mins)		Temp. C

0			20

2			55.7

5			67.8

Particle Size			Millimetres		Passing %		Passing Range %

5.00			100			95 - 100

3.35			100

1.00			85.1

Bulk Densities			kg/m3			990

Finelime® quicklime conforms to BSEN 459-1: 2010 Building Lime as CL 90-Q (R5, P4) and is CE marked (MR certificate number 0785-CPR-11168-13 / BC certificate number 0785-CPR-11265-13)

This specification relates to product numbers: 	124003 - Bulk (MR)		Last Revision Date: July 2013

124503 - IBC500 (MR)

124203 - Bulk (BC)

Storage Recommended minimum bulk silo capacity for quicklime/aqualime® 60m3, Ultralime® 120m3.

Further advice/information available on request.

Safety 	Refer to our Safety Data Sheet.