Natural Hydraulic Lime 3.5

EN 459-1:2010 NHL3.5

Natural Hydraulic Lime is a fine, off-white powder which is made by the calcination of specially selected siliceous chalks or limestone.

Chemical Characteristics					Value			Standard

Free Lime - Ca(OH)2		%			 ≥ 25.0			EN459-1

Sulphate - SO3			%	  		 ≤ 2.0			EN459-1

Physical Characteristics

Colour							Beige			-

Specific Mass			kg/dm3			0.65 ± 0.05		EN459-1

Density				kg/m3			675			-

Fineness - 90µm		%			≤ 15.0			EN459-1

Fineness - 200µm		%			≤ 2.0			EN459-1

Blaine				cm2/g			9000			-

Expandability			mm			≤ 20			EN459-1

(alternative method)

Free Water			%			≤ 2.0			EN459-1

Air content			%			≤ 5			EN459-1

Penetration			mm			>10 and <50		EN459-1

Setting Time 	(Initial)		Hrs			> 1.0			EN459-1

Setting Time 	(Final)		Hrs			≤ 30.0			EN459-1

Mechanical Characteristics

Mechanical Compressive

28 Days			N/mm2	(MPa)		≥ 3.5 ≤ 10.0		EN459-1

This product conforms to BSEN 459-1: 2010 Building Lime as a NHL3.5 and is CE marked (certificate number 1328-CPR-0215)

This specification relates to product numbers: 	171103 - BAG25				Last Revision Date:July 2014

Storage Recommended minimum bulk silo capacity for quicklime/Aqualime® 60m3, Ultralime® 120m3.

Further advice/information available on request.

Safety 	Refer to our Safety Data Sheet.