Natural Hydraulic Lime 5

EN 459-1:2010 NHL5

Natural Hydraulic Lime is a fine, off-white powder which is made by the calcination of specially selected siliceous chalks or limestone.

Chemical Characteristics					Value			Standard

Free Lime - Ca(OH)2		%			 ≥ 15.0			EN459-1

Sulphate - SO3			%	  		 ≤ 2.0			EN459-1

Physical Characteristics

Colour							Beige			-

Specific Mass			kg/dm3			0.65 ± 0.05		EN459-1

Density				kg/m3			700			-

Fineness - 90µm		%			≤ 15.0			EN459-1

Fineness - 200µm		%			≤ 5.0			EN459-1

Blaine				cm2/g			9400			-

Expandability			mm			≤ 20			EN459-1

(alternative method)

Free Water			%			≤ 2.0			EN459-1

Air content			%			≤ 5			EN459-1

Penetration			mm			>10 and <50		EN459-1

Setting Time 	(Initial)		Hrs			> 1.0			EN459-1

Setting Time 	(Final)		Hrs			≤ 15.0			EN459-1

Mechanical Characteristics

Mechanical Compressive

7 Days				N/mm2	(MPa)		≥ 2.0			EN459-1

28 Days			N/mm2	(MPa)		≥ 5.0 ≤ 15		EN459-1

This product conforms to BSEN 459-1: 2010 Building Lime as a NHL5 and is CE marked (certificate number 1328-CPD-0215 )

This specification relates to product numbers: 	173103 - BAG25				Last Revision Date: July 2014

Storage Recommended minimum bulk silo capacity for quicklime/Aqualime® 60m3, Ultralime® 120m3.

Further advice/information available on request.

Safety 	Refer to our Safety Data Sheet.